## Slide 1
FeFET in 22nm FDSOI for fast, low-power, non-volatile memory
Presentation by:
Khalil Ouali
Khumar Huseynzade
Olya Tsormutyan
Nanotechnology course — Dr. Andreas Bablich
Winter Semester 2025-2026

## Slide 2
High-Capacity Non-Volatile Memory [5][3]
Floating Gate (Poly) or Charge Trap Layer (SiNₓ)
Tunnel Oxide
p-substrate
Drain (n⁺)
Source (n⁺)
Inter-Poly Dielectric
Control Gate
(Poly)
Simplified Floating-Gate FET operation in traditional flash memory
Low Voltage
High/Low Drain Current
Read
Program / Erase
± Large Voltage
± Charge Storage
Limitations:
⚡ High Power Consumption
🕝 Slow Speed
📉 Quick Degradation
💰 High Cost
☢️ Radiation Susceptibility
Limited Applications:
📱 Embedded and IOT 🌐
🛰️ Space and Nuclear ⚛️
⇒ Alternative: FeFET
Notes: Program/erase: ±8-12V
Power consumption: high voltage and some current for charge/discharge
Tradeoff between power and speed, and between speed and endurance, depending on voltage
High cost due to complex process integration
Cosmic ionizing radiation can charge/discharge a cell spontaneously, corrupting data

## Slide 3
Ferro
HK
Channel
S
G
D
Operation Principle
Simplified FeFET structure
Simplified visualization of ferroelectric crystal polarization
Hysteresis curve of ferroelectric polarization as a function of voltage
FeFET drain current as a function of gate voltage
👆 Click here to visit Desmos link (online animation)
Notes: Oxygen is highly electronegative; electrons stick to it.
It has 2 stable positions. Enough force (electric field) can snap it to another position.

## Slide 4
FeFET states [1]
Ferroelectric Si:HfO₂ : Fabrication and Polarizations [2]
Operation Principle
Polarization hysteresis in ferroelectric Si:HfO₂[3]
Hysteresis in FeFET transfer curve [1]
Notes: Voltage: High + → program, High - → erase, Low → read

## Slide 5
Si
SiO₂
Si wafer with ultra thin body and buried oxide (UTBB)
After cleaning, padding, Shallow Trench Isolation (STI)
Fabrication [1][2][3][4][Course][+]
BOX
Notes: Moving onto the fabrication of the device, we don't have exact details about the process since it's proprietary, but this is our best inference based on various sources including our course.
This device is fabricated in a Fully-Depleted Silicon-on-Insulator process, so we will need a buried oxide, and unlike regular SOI, we will keep the body silicon layer very thin and without channel doping, such that the depletion regions from the drain and source cover the entire channel length.
We will skip a few steps that aren't very relevant to our device like the wafer preparation, box implantation, and shallow trench isolation.
--
Buried oxide ← ion implantation followed by anneal
Silicon thickness = 5-10nm

## Slide 6
Rapid Thermal Oxidation (RTO) + Nitridation (RTN)
⇒ Interfacial layer (IL)
Si
SiO₂
SiON
BOX
! Gate First process
! Fully-Depleted SOI doesn't require channel doping
Notes: This is a gate-first process, so we will deposit the full gate stack and pattern it later, starting with a thin interfacial layer done by rapid thermal oxidation and nitridation.
---
Advantage of gate-first: thermal budget as doping happens later so diffusion isn't as harmful

## Slide 7
HK
Atomic Layer Deposition (ALD) of Si:HfO₂
→ Amorphous, lightly-doped, High-K dielectric (HK)
Si
SiO₂
Si:HfO₂
SiON
BOX
! Additional masks to select FeFETs vs logic FETs
Notes: Next, we use atomic layer deposition to grow an amorphous layer of high-k dielectric hafnium dioxide with light silicon doping.
During this step, we require additional masks to select different FETs, logic or ferroelectric, and deposit accordingly.

## Slide 8
ALD / Physical Vapor Deposition (PVD) of TiN
⇒ Metal gate
MG
Si
SiO₂
Si:HfO₂
SiON
TiN
HK
BOX
Notes: Over the HK layer we deposit the gate metal, Titanium Nitride, using PVD (or ALD again).

## Slide 9
Rapid Thermal Annealing (RTA) → Encapsulated Si:HfO₂ Crystallization
⇒ Ferroelectric HK
Si
SiO₂
Si:HfO₂
SiON
TiN
MG
Ferro-HK
BOX
Notes: One critical detail is that we need to crystallize the HK using rapid thermal annealing after the metal deposition, and not before.
The light silicon doping, combined with the encapsulation, is what crystallizes the material into a ferroelectric phase.

## Slide 10
Low Pressure (LP) Chemical Vapor Deposition (CVD) of Poly-Si
Poly-Si
Si
SiO₂
Si:HfO₂
SiON
TiN
MG
Ferro-HK
BOX
Notes: Next, we finish the gate stack with the low-pressure chemical vapor deposition of a poly-crystalline silicon layer.

## Slide 11
MG
Photolithography + Multi-Step Reactive Ion Etching (RIE)
⇒ Gate Patterning
Poly-Si
Ferro-HK
Si
SiO₂
Si:HfO₂
SiON
TiN
BOX
Notes: We pattern the gates using photolithography and multi-step reactive ion etching.

## Slide 12
MG
Ion Implantation of P / As / Sb → Low N-type doping
⇒ Lightly-Doped Drain (LDD) and Source
Channel
n⁻
n⁻
Poly-Si
Ferro-HK
Si
SiO₂
Si:HfO₂
SiON
TiN
BOX
Notes: After which we do light N-doping for the lightly doped drain and source
--
Phosphor / Arsenic / Antimony

## Slide 13
MG
Channel
n⁻
n⁻
Poly-Si
Ferro-HK
Si
SiO₂
Si:HfO₂
SiON
TiN
LPCVD of Undoped Silicate Glass (USG) and/or Nitride
+ RIE ⇒ Sidewall Spacers
BOX
Notes: We add the sidewall spacers using LPCVD and anisotropic reactive ion etching.

## Slide 14
BOX
MG
Selective Epitaxy with In-Situ N-Type Doping of P + RTA
⇒ Raised Source & Drain
Channel
n⁻
n⁻
n⁺
Poly-Si
n⁺
Ferro-HK
Si
SiO₂
Si:HfO₂
SiON
TiN
Notes: Then we do selective epitaxy with in-situ N-type doping in order to create raised source and drain
--
Raised source and drain advantage: Reduced series resistance and additional volume for silicidation
P: Phosphorus
Selective epitaxy with in-situ doping is essentially CVD.

## Slide 15
Ferro-HK
BOX
MG
PVD of Ni + Annealing + Unreacted metal strip
⇒ Self-aligned Silicide (Salicide)
Channel
n⁻
n⁻
n⁺
Poly-Si
n⁺
NiSi
Si
SiO₂
Si:HfO₂
SiON
TiN
Silicide
Silicide
Silicide
Notes: After using PVD for Nickel deposition, annealing, and etching unreacted metal, we get a salicide layer for each contact
--
Low-temp anneal
Strip: wet etch
Silicide advantage: low contact resistivity

## Slide 16
PSG
PSG
Ferro-HK
BOX
MG
CVD of Phospho-Silicate Glass (PSG) + Photolithography + W + CMP
Channel
n⁻
n⁻
n⁺
Poly-Si
n⁺
P:SiO₂
W
NiSi
Si
SiO₂
Si:HfO₂
SiON
TiN
W Plug
W Plug
Silicide
Silicide
Silicide
Notes: Finally, we finish with the PSG deposition, Tungsten plugs, and final cleanup, thus arriving at the final structure.

## Slide 17
22nm FeFET TEM cross-section [1]
Final Structure
PSG
PSG
Ferro-HK
BOX
MG
Channel
n⁻
n⁻
n⁺
Poly-Si
n⁺
W Plug
W Plug
Silicide
Silicide
Silicide

## Slide 18
Process Integration
TEM cross-sections of 22nm FDSOI FeFET and logic FETs [1]
22nm FDSOI base process flow [4]
SEM of 28nm embedded FeFET NVM border [3]
Logic FET performance in 22nm FDSOI with and without FeFET integration [1]
Notes: - The fabrication of these devices was successfully integrated into a commercial FDSOI CMOS process called 22FDX that is offered by global foundries.
- On the top right you can see TEM cross-sections of an nmos and pmos fabricated on the same die.
- On the left we have a scanning electron micrograph of the die, but for 28nm node, highlighting the separation between the FeFET region with Ferro-HK, and standard logic FETs with normal HK.
-The flow diagram in the middle presents the original 22nm process excluding the FeFET specific steps, but the paper mentions that only 2 mask additions are required, presumably for the FET selection.
- And the integration is non-invasive, as shown in this graph on the right, the performance of the logic FETs essentially doesn't change with the addition of the FeFET steps.
---
Orange parts:
- SiGe channel and Dual-epi for improved pMOS performance in FDSOI,
- Hybrid (well taps) because this process actually combines FDSOI and non-SOI (just bulk silicon) for maximum flexibility,
- Metal 1 and 2 patterning offers more control over those two metal layers (not sure what for exactly)

## Slide 19
Back-Biasing
FeFET structure incl. back-biasing [1]
Effect of back-biasing on transfer curve[1]
Effect of back-biasing on threshold voltages [1]
Performance
Low- and high-Vₜ (±3.8V, 10μs) transfer curves of a 80x20nm FDSOI FeFET [1]
Notes: Back-biasing shifts both threshold voltages in the same direction, barely affecting the window size.
Vbb applied to substrate (bulk), and produces a field effect like the gate.
It has the same effect as the gate voltage (not unlike gate-all-around) but much weaker. +Vbb attracts electrons, helps form channel, lowering Vth, and vice-versa.

## Slide 20
Memory Array Testing
Drain current (↑) and bit (↓) readouts after writing checkerboard and complex patterns
in a 0.036μm² cell 32MBit array [1]
Memory array test circuit [1]
FeFET logic yield, limited mainly due to defects [1]
Notes: Bit error rate is how many bits of the programmed pattern were wrong when read back

## Slide 21
Size vs Performance
Memory window and variation for FeFETs with different device dimensions [1]
Threshold voltage distribution for different sizes [1]
Notes: At smaller sizes, memory window shrinks and variation increases, which is bad

## Slide 22
Endurance
Bipolar endurance cycling (±3.5V, 10μs) of a 170x24nm FeFET [1]
Retention measurement of 0.28μm² cell 64 kBit array @ 250 °C [1]
Retention measurement of 0.28μm² cell 64 kBit array @ 300 °C after 1 h [1]
Charge trapping, counteracting the ferroelectric polarization [3]
Notes: Issues at the interface cause ion migration and charge trapping in the high-K, narrowing the memory window
250°C: most degradation happens in the first few minutes, then stabilizes somewhat
300°C: the heat had similar effects on both threshold voltages, so memory window doesn't shrink too much

## Slide 23
Comparison with Flash (28nm)
Prospects of hafnium-based FeFET eNVM for the ‘Generation 1’ flow vs. best projected values taken from the ITRS and embedded Flash. [3]
🕝 Speed
⚡ Power
☢️ Radiation
💰 Cost
📉 Durability
Notes: Power consumption not exactly quantified, but confirmed to be lower than flash

## Slide 24
References
[1]
S. Dünkel et al., “A FeFET based super-low-power ultra-fast embedded NVM technology for 22nm FDSOI and beyond,” in 2017 IEEE International Electron Devices Meeting (IEDM), Dec. 2017, p. 19.7.1-19.7.4. doi: 10.1109/IEDM.2017.8268425.
[2]
T. S. Böscke, J. Müller, D. Bräuhaus, U. Schröder, and U. Böttger, “Ferroelectricity in hafnium oxide thin films,” Appl. Phys. Lett., vol. 99, no. 10, p. 102903, Sept. 2011, doi: 10.1063/1.3634052.
[3]
M. Trentzsch et al., “A 28nm HKMG super low power embedded NVM technology based on ferroelectric FETs,” in 2016 IEEE International Electron Devices Meeting (IEDM), Dec. 2016, p. 11.5.1-11.5.4. doi: 10.1109/IEDM.2016.7838397.
[4]
R. Carter et al., “22nm FDSOI technology for emerging mobile, Internet-of-Things, and RF applications,” in 2016 IEEE International Electron Devices Meeting (IEDM), Dec. 2016, p. 2.2.1-2.2.4. doi: 10.1109/IEDM.2016.7838029.
[5]
R. Bez, E. Camerlenghi, A. Modelli, and A. Visconti, “Introduction to flash memory,” Proceedings of the IEEE, vol. 91, no. 4, pp. 489–502, Apr. 2003, doi: 10.1109/JPROC.2003.811702.

## Slide 25
Thank you
for your attention